Series PRE

PRESSURE REGULATORS

INSTALLATION & MAINTENANCE INSTRUCTIONS

IMPORTANT - BEFORE INSTALLING

Series PRE pressure regulators will prevent downstream pressure from exceeding the set pressure, when properly installed and used within the recommended ranges of pressure, temperature, and chemical compatibility.  The ultimate determination of material compatibility is previous successful use in the same application. See the Product Data Sheet or call our Technical Support for information about your application.

Caution: Plastic materials will degrade in ultraviolet (UV) light or sunlight.

Caution: Polypropylene and PVDF (Kynar) often look similar. Do not install in your system if you are not sure.

Caution: Quick closing valves installed downstream of the regulator may cause water hammer.  This may cause leakage or seal damage.

RATINGS

Inlet pressure 	150 PSI at 75°F  (10 Bar at 25°C)

Outlet pressure	125 PSI at 75°F	 (  8 Bar at 25°C)

INSTALLATION

Install the valve in the proper flow direction as indicated by the flow label.  The valve may be set vertically or horizontally.

THREADED CONNECTION - Apply a suitable thread sealant (for example, PTFE tape) to male tapered threads to assure a “leak-tight” seal.  Assemble “hand-tight” followed by a quarter (1/4) turn with a strap wrench.  Do not over tighten or use pipe wrenches on plastic pipe and components.

Caution: PTFE tape will “string” as pipe threads are joined.  Loose “strings” could lie across the seating surface and prevent the valve from completely closing.  To avoid this problem, clean out old tape, and do not apply tape to the first thread.

Caution: Connect to plastic pipe and fittings only; when using metal pipe, install an intervening plastic fitting.  Metal pipe and straight threaded pipe tends to cut, stretch, and distort the plastic bodies, resulting in cracking or leaking over time.

NON-THREADED CONNECTIONS - For solvent cementing or heat fusion, follow the instructions supplied with the cement or fusion equipment, or contact your distributor.

MOUNTING - These valves are designed to be supported by the piping.  The piping must be properly supported, taking into account the weight of the valve, piping, and process liquid.

PRESSURE SETTING

Install the valve.  Turn the adjusting screw all the way out.  With the inlet at a pressure above the desired point and the system operating normally, turn the adjusting screw in to reach the desired outlet pressure.  Lock the pressure setting by tightening the nut on the adjusting screw assembly.

MAINTENANCE

Plast-O-Matic recommends keeping a spare seal kit available for repairs.  Seal life will vary in applications due to cycles, temperatures, pressures, chemicals, and concentration. Based on the application, a periodic inspection and maintenance plan should be established.  The seal kit part number is “SK” plus the part number less the material suffix.  For example, the seal kit for PRE050V-PV is SKPRE050V.